	
The following list shows the chemical composition of the plastic clay suitable for production of LECA.
average value 

variation band 

xsilicium dioxide 

SiO2 

55.0 % 

48.0-65.0% 

xiron oxide 

Fe2O3 

7.5 % 

1.0-10.0% 

xaluminium oxide 

Al2O3 

17.5 % 

14.0-22.0% 

xcalcium oxide 

CaO 

2.0 % 

0-5.0% 

xmagnesium oxide 

MgO 

2.5 % 

0-4.0% 

xsodium oxide 

Na2O 

1.0 % 

0-2.5% 

xpotassium oxide 

K2O 

3.5 % 

2.0-4.0% 

xtitanium dioxide 

TiO2 

1.1 % 

0.7-1.5% 

xsulphur trioxide 

SO3 

indication 

h
xchloride 

Cl 

indication 

h
xignition loss 

h
8.5 % 

4.0-15.0% 

 


